

**emco Bau**

Clean-off system OUTDOOR

|  |  |
| --- | --- |
| **Model** | OUTDOOR |
|  | For outdoor use |
| **Construction** | 5/32'’ tufting |
| **Pile above substrate** | 100% polyamide |
| **Substrate material** | Polyester fleece |
| **Backing material** | Heavy coating |
| **Pile weight / fibre weight** | 600 g/m² |
| **Total weight (g/m²)** | 3200 g/m² |
| **Overall height (mm)** | 8 mm |
| **Combustion/fire behaviour** | Cfl-s1 |
| **Slip resistance** | DS (EN 13893) |
| **Certificates** | CE conformity EN 14041 (rolls only) |
| **Colours** | Anthracite |
|  | Brown |
|  | Red |
| **Colour fastness to artificial light ISO 105-B02** | ≥7 |
| **Colour fastness to rubbing ISO 105 X12** | ≥4 |
| **Colour fastness to water ISO 105 E01** | ≥4 |
| **Bacterial reduction EHEC ASTM-e2149** | 22,4 % |
| **Bacterial reduction staphylococcus aureus ASTM-e2149** | 17,3 % |
| **Bacterial reduction klebsiella pneumoniae ASTM-e2149** | 9,8 % |
| **Supplied as rolls** | 100 cm wide (incl. border) |
|  | 200 cm wide (incl. border) |
| **Supplied as mats** | 60 x 90 cm (incl. border) |
|  | 90 x 150 cm (incl. border) |
| **Product characteristics** | Soiling and moisture absorption |
| **Brand** | emco |
| **Dimensions** | Width:.........................m |
|  | Length:.........................m |
| **Contact** | emco Bautechnik GmbH · Memeler Straße 30 · D-42781 Haan Germany · Tel.: +49 (0)21 29/34 75 80 · Telefax: +49 (0)21 29/34 75 810 E-Mail: sauberlauf@emco.de · www.emco-bau.com |